## Slide 1: Data Analysis with LAMPS
Description of Data Input and Output during SLS build process

## Slide 2: Introduction LAMPS
General Information
Laser Additive Manufacturing Pilot System (LAMPS)
SLS testbed designed and built at UT Austin for process control research
Open Architecture Software allowing access to all process parameters
Enable examination of polymers up to PEEK/PAEK/PEKK class: (Process temps as high as 350 C)
Provide In-situ measurement access

## Slide 3: Introduction LAMPS
Sensors and Actuators implemented in LAMPS
Sensors
  2 x MWIR Cameras
  1 x Visual Camera
  > 50 Thermocouples
  1 x Optical Coherence Tomography (OCT) System
Actuators
  1 x Laser with 2 axis Galvometers
  3 x Quartz Lamps
  > 10 Strip Heaters
  Piston height adjustment (layer thickness)
  Powder spreading roller (translation and rotation independent control)
  Nitrogen flow rate (manual valve control, can be other gas) and pre-heating
1
1, 4
2
5
6
7
3
9

## Slide 4: Sensors and Actuators
Data produced by Sensors – Powderbed IR camera & Thermocouples
6701 MWIR (30 – 60 Hz currently used framerate)
  Up to 126 Hz in full window mode (640 x 512 pixels)
  Provides multiple Region of Interest (ROI) mean for
    Drop zone
    Build Surface (1 Hz)
  ROI temperatures used to control quartz lamp powers
  Provides real-time video for user monitoring
Thermocouples (1-2 Hz)
  Locations
    Chamber walls
    Chamber atmosphere
    Build box / piston walls and optional manual insertion into powder
6701 MWIR IR image

## Slide 5: Sensors and Actuators
Data produced by Sensors – Boresighted & Visual Camera
FLIR SC8240 IR camera
  Up to 2,243 Hz framerate at 64x64 pixels, area of pixel is roughly 300 x 340 microns
  132 Hz frame rate for full window (pixels?)
  Boresighted with CO₂ laser
  Typically used in conjunction with laser action (prior to or during laser scans)
Visual camera
  Takes 1 image before roller spread and 2 images after spread
  Provides real-time video of the powder bed for user monitoring (user evaluation of powder spreading quality, or other surface/part movement anomalies)
FLIR SC8240 IR image

## Slide 6: Sensors and Actuators
Data produced by Sensors - Optical coherence tomography (OCT)
OCT measurements (100 kHz sample rate)
  Established non-invasive, high resolution medical imaging technique
  Produces cross-sectional and 3D representations of sample
  Data volume dependent on experimental requirements (do we have an idea what a typical B scan data volume is?)

## Slide 7: Sensors and Actuators
Communication with Actuators
Laser with Galvometers
  EC 1000 controls Galvometers and Laser
  Interface with LabVIEW
  Communicates through XY2 100 protocol (updates at 100 kHz)
Quartz Lamps
  Updated continuously (30 Hz or 60 Hz according to camera framerate)
Strip Heaters
  Currently updated at 100 Hz, likely to be reduced to 10 Hz
EC 1000

## Slide 8: Data Flow during Build
Flow Diagram for Standard Builds
CAD
STL file
LabVIEW - Startup
Slicer (specifies layer thickness)
1 Outline txt file per layer (same folder)
Configuration File (.xml):
Sets temperatures for QL and Heaters
(…>trunk>LAMPS_Config_Files)
1 Infill txt file per layer (USB drive or …>documents>builds)
EC1000 prompt (input laser parameters)
Front panel control (Infill and Outline power)
Start build
(prompt asks for infill and outline txt file location)
Required Files
External Hard drive “Backup”
Recorded for each layer (always the same though)

## Slide 9: Data Flow during Build
LabVIEW – Data Flow during Build
Flow Diagram for Standard Builds
Quartz Lamps
Strip Heaters
IR
External Hard drive “Backup”
Thermocouples
Config file
Visual Diagnostics
Current TC readings
TC over time
ROI graph
TC and DC of QL over time
Thermal Camera
Feedback with IR readings from powder bed
Visual Camera
.xlsx
binary
.tot
.xlsx
EC 1000
Laser & Galvos
Sample rate set in LV?
LabVIEW
LabVIEW - Cooldown
Cooldown activated by front panel control button
Input Cooldown config files (same folder as prev. config files

## Slide 10: Data Flow during Build
OCT Data
Single Scan Line Test Video
Each frame ≈ 0.03 seconds
Click on Video to play it.
OCT image on the right is B-Scan of the powder before and after the laser melted a line horizontally
Image shows a B-scan which consists of ca. 7000 A-scans (each A-scan is a column)

## Slide 11: Data Flow during Build
OCT Data I/O
Required data for OCT measurement
  Set OCT parameters
      set data collection time (how long)
      Specify file storage location
OCT doesn’t require extra information during build, it will record for the time specified
As of now, OCT is not used in any control loop  build will process regardless of OCT measurement
What data is recorded during the build for either diagnostics or post build analysis?
  Raw data is stored in a binary file in the storage location specified
  OCT parameters are stored in a text file in the same storage location